2304 – 119 Avenue NE

Edmonton, Alberta

T6S 1B3

March 6, 2026

File No. 5478 – 1

VICTORY HOMES LTD.

1665 – 91 Street SW
Edmonton, Alberta
T6X 0W8

Re:	Foundation Soil Inspection – Garden Suite

Lot 110, Block 17, Plan 252 2250

607 – 30 Street SW

Alces Subdivision

Edmonton, Alberta

As requested, J.R. Paine & Associates Ltd., (JRP), has conducted an inspection of the above noted excavation on March 5, 2026.  The purpose of this inspection was to verify that the site soil bearing capacity and expected settlement are adequate to support typical house loads, and where they are not adequate, to recommend a foundation design to address these bearing and settlement issues.  It is assumed that this house is designed and will be constructed in accordance with the Alberta Building Code, except where superseded by this letter.

At the time of inspection, the excavation was at footing grade and was advanced by a backhoe.  Cuts of approximately 1.2 to 1.7 m below the adjacent ground surface were noted.

The soil encountered throughout the excavation floor to a depth of approximately 0.3 m was identified as moist, brown/dark grey, silty, sandy clay fill. The fill material was a native deposit of medium to high plasticity with a very stiff consistency and contained traces oxides, and organics. Below the fill, moist, brown, silty, sandy clay till was encountered. The till material was a native deposit of medium plasticity with a stiff consistency and featured trace amounts of oxides, coal and gravel.  This lot was part of an engineered fill program monitored and tested by our firm. The high plastic clay is highly susceptible to shrinkage and swelling with changes in moisture content and may undergo movement over time.  Please contact our firm for further input if desired.

The soil conditions at this site were considered adequate for the construction of a rear garage garden suite structure. A minimum strip footing width of 450 mm and a minimum depth of 150 mm are recommended for the rear garage garden suite structure. Also, a minimum cover of 2.0 m for frost protection should be provided for non-continuously heated structures or exterior isolated footings.  The frost cover can be reduced to 1.5 m for continuously heated structures.  As an option, frost cover can be obtained by the use of exterior rigid insulation.  Insulation details can be supplied upon request.

During cold weather construction, it is essential that all interior fill and load bearing material remain as frost free as possible.  In order to minimize the potential frost heave problems, the interior of the building must be heated as soon as the walls have been poured and the sub-floor is placed.  The period in which the excavation is left open to freezing conditions should be as short as possible.  There must be no delays from the time of excavation to the placement of the temporary heat system.  Recommended cold weather construction practices, with respect to hoarding and heating of the forms and the fresh concrete, should be followed.

We trust this information is considered satisfactory.  Should you have any questions, please contact our office.

Yours truly,

J.R. Paine & Associates Ltd.

Muhammad Huzaifa, E.I.T.

Reviewed by,

Scott MacFarlane, P.Eng.

APEGA Member #: 89667

H:\DATA 2026\00 Housing 2026\5478-1 Victory Homes Ltd\h38733vic.docx