2304 – 119 Avenue NE

Edmonton, Alberta

T6S 1B3

February 27, 2026

File No. 5478 – 1

VICTORY HOMES LTD.

1665 – 91 Street SW
Edmonton, Alberta
T6X 0W8

Re:	Foundation Soil Inspection

Lots 60, Block 3, Plan 252 2509

4220 – 63 Street

Ruisseau Subdivision

Beaumont, Alberta

As requested, J. R. Paine & Associates Ltd., (JRP), has conducted an inspection of the above noted excavation on February 26, 2026.  The purpose of this inspection was to verify that the site soil bearing capacity and expected settlement are adequate to support typical house loads, and where they are not adequate, to recommend a foundation design to address these bearing and settlement issues.  It is assumed that this house is designed and will be constructed in accordance with the Alberta Building Code, except where superseded by this letter.

At the time of inspection, the excavation was at footing grade and was advanced by a backhoe.  Cuts of approximately 1.3 to 1.9 m below the adjacent ground surface were noted. An excavation had also been made in the garage footing area, which was level with the house excavation floor.  An extra 1.2 metres of material was to be removed from the back portion of the excavation to allow for the construction of a frost wall to accommodate a rear walkout basement.

The soil encountered throughout the excavation floor was identified as moist, grey and brown, silty sandy clay till.  The clay till material was a native deposit of medium plasticity with a very stiff consistency and contained traces of coal, oxides and gravel.

The soil conditions at this site were considered adequate for the construction of a standard house footing foundation.  A minimum strip footing width of 450 mm and a minimum depth of 150 mm are recommended. Spread footings may be designed utilizing a factored bearing resistance of 140 kPa (2900 pounds per square foot) with a geotechnical resistance factor of 0.5.

It is understood the building contractor wishes to utilize a standard footing foundation for the attached garage.  A minimum strip footing width of 450 millimetres and a minimum depth of 150 millimetres are recommended for the garage. Also, a minimum cover of 2.0 metres for frost protection should be provided for non-continuously heated structures or exterior isolated footings.  The frost cover can be reduced to 1.5 metres for continuously heated structures.  As an option, frost cover can be obtained by the use of exterior rigid insulation.  Insulation details can be supplied upon request.

During cold weather construction, it is essential that all interior fill and load bearing material remain as frost free as possible.  In order to minimize the potential frost heave problems, the interior of the building must be heated as soon as the walls have been poured and the sub-floor is placed.  The period in which the excavation is left open to freezing conditions should be as short as possible.  There must be no delays from the time of excavation to the placement of the temporary heat system.  Recommended cold weather construction practices, with respect to hoarding and heating of the forms and the fresh concrete, should be followed.

We trust this information is considered satisfactory.  Should you have any questions, please contact our office.

Yours truly,

J.R. PAINE & ASSOCIATES LTD.

Doug Parth, E.I.T.

Reviewed by,

Patrick Winski, P.Eng.

APEGA Member #71849

H:\DATA 2026\00 Housing 2026\5478-1 Victory Homes Ltd\h38696vic.docx